EXECUTIVE SUMMARY OF THE THESIS

Synthesis of new bipyridine and phenantroline based ligands for the separation of americium from the active PUREX raffinate

TESI MAGISTRALE IN CHEMICAL ENGINEERING – INGEGNERIA CHIMICA

AUTHOR: FABRIZIO PIROMALLI

ADVISOR: ALESSANDRO SACCHETTI

ACADEMIC YEAR: 2022-2023

# Introduction

One of the problems that nuclear power must face is the management of the radioactive waste leaving the nuclear reactor. Various processes that can separate the various radioactive elements for better waste management have been developed. The existing processes are aimed at separating elements that are reusable as fuel from those that are considered waste. After PUREX, a well-established process that allows the recycling of uranium and plutonium, a series of processes follow which aim at the separation of americium from radioactive waste for its recycling in the reactor. The main issue in fulfilling the separation of americium from the other elements is the chemical and physical similarity with curium [1] [2] [3].

Nowadays, a process aimed at the direct separation of americium from the PUREX raffinate, the AmSel (Americium Selective Extraction) process, is under development. The AmSel process exploits the inverse selectivity for Am (III) showed by the lipophilic ligand TODGA, present in the organic phase, and the hydrophilic complexing agent sulfonated BTBP, dissolved in the aqueous phase [4].

# Aim of the work

The aim of thesis is to synthetize new ligands that have almost the same performance of the sulfanated ligand SO3-Ph-BTBP while being CHON, so they do not have atoms other than carbon, hydrogen, nitrogen and oxygen in their molecular structure. This allows the complete combustion of the ligands without producing solid ashes but only gaseous products.

To achieve this goal, the work is focused on the search of the molecular structure that allows to better complex americium, by means of a complexing core, while keeping it in the aqueous phase, by means of the side chains. So, the chemical synthesis of the ligands and their performance evaluation of their ability in complexing are the key steps of the work. Performance evaluation is performed by introducing the synthesized ligands into an environment reproducing the operating conditions of the AmSel process.

# Experimental activities

The experimental activities of the thesis are divided in two parts:

- The chemical synthesis of the ligands.

- The performance evaluation of the ligands

# 3.1 Chemical synthesis

Two different kinds of ligands were synthetized based on the different core structure. Two bipyridine based ligands that have a flexible complexing core and a phenantroline based ligand that has a rigid core structure have been synthetized. The different choice of the structure of the complexing core influences the complexing selectivity of americium complexation.

The proposed ligands (Figure 1) that aim at substituting SO3-Ph-BTBP are:

- 3,3'-(4,4'-([2,2'-bipyridine]-6,6'-diyl) bis(1H-1,2,3-triazole-4,1-diyl))bis(propane-1,2-diol) (shortened as propane-1,2-diol-BTzBP).

- 2,2'-(((4,4'-([2,2'-bipyridine]-6,6'-diyl) bis(1H-1,2,3-triazole-4,1-diyl))bis(ethane-2,1-diyl))bis(oxy))diethanol (shortened as ethoxyethanol-BTzBP)

- 2,2'-(((4,4'-(1,10-phenanthroline-2,9-diyl) bis(1H-1,2,3-triazole-4,1-diyl))bis(ethane-2,1-diyl))bis(oxy))diethanol (shortened as ethoxyethanol-BTzPhen)

Figure 1: ligands’ molecules

a) propane-1,2-diol-BTzBP

b) ethoxyethanol-BTzBP

c) ethoxyethanol-BTzPhen

The synthesis of ligands occurs first by synthesizing the side chains. Subsequently these are made to react with the complexing nucleus with the formation of the triazole side ring.

The synthesis of the side chains is reported in Figure 2:

a)

b)

Figure 2: Side chains’ synthesis

- Synthesis of 3-azidopropane-1,2-diol

- Synthesis of 2-(2-azidoethoxy) ethanol

After the side chains synthesis, intermediate steps of core’s functionalization are required in order to carry out the click reaction that allow to attach the side chains to the core of the ligand. The functionalization of the complexing cores is performed through a Sonogashira reaction in the case of the bipyridine and through an oxidation followed by a reaction with the Bestmann-Ohira reagent in the case of the phenantroline. The functionalization reactions are:

a)

b)

c)

Figure 3: Cores’ functionalization reactions

- Sonogashira reaction undergone by a bipyridine

- Oxidation reaction of the phenantroline core preliminary to functionalization

- Phenantroline functionalization with the addition of the Bestmann-Ohira reagent

Now the cores and the side chains are ready to undergo the click reactions, forming the proposed ligands. The click reactions are reported in Figure 4:

Figure 4: click reaction between the functionalized core and the side chain leading to:

  - propane-1,2-diol-BTzBP

  - ethoxyethanol-BTzBP

  - ethoxyethanol-BTzPhen

# 3.1.1 Products’ purification

Many purification techniques were exploited to purify the intermediate products such as column chromatography, washing, solvent extraction etc. The products of the click reactions were purified through an organic solvent extraction (DCM) and filtration.

# 3.3 Ligands characterization

Characterization analyses were done to ensure the quality of the product and to gain more knowledge about it. The techniques used to perform the characterization are:

DFT (Density - Functional Theory) computational analysis.

Single crystal X-ray diffraction.

The results were useful to understand the complexation mechanism.

# 3.3 Ligand’s performance evaluation

The tests were designed to simulate the AmSel process which consists of a liquid-liquid extraction between an aqueous and an organic phase (batch tests).

The proposed ligands must be hydrophilic so, before undergoing the batch extracting test, a solubility test on these must be carry out.

The extracting test is carried out by contacting 200 μL, containing the organic extractant TODGA, with 200 μL of aqueous phase containing the ligand and the solution of radioactive tracer that simulates PUREX raffinate metals’ composition. Once the system has reached the equilibrium, the resulting composition of the radioactive metals in the aqueous and in the organic phases is investigated through gamma and alpha analysis. The extracting system is reported in Table 1.

Table 1: composition of the aqueous and organic phases in the batch tests

# 4. Analysis of the results

# 4.1 Ligands’ solubility

Ethoxyethanol-BTzBP and ethoxyethanol-BTzPhen showed very good solubility even at low acidic conditions.

Propane-1,2-diol-BTzBP displayed an unexpected very low solubility, so few tests at low ligands’ concentration were carried out.

# 4.2 Extracting performance

While propane-1,2-diol-BTzBP gave very bad values of distribution factor of americium, ethoxyethanol-BTzBP (Figure 5) and ethoxyethanol-BTzPhen performances seem to be very promising. Due to the lack of time, few test were carried out on all the ligands, so no optimum acidity conditions were identified.

As it can be observed in Figure 6, the ethoxyethanol-BTzPhen seems to be very promising in terms of extracting performance, resulting a valuable alternative to the SO3-Ph-BTBP. This good ability in complexing americium is maybe due to the rigid configuration of the phenantroline.

Figure 5: Distribution factors in presence of ethoxyethanol-BTzBP

Figure 6: Distribution factors in presence of ethoxyethanol-BTzPhen.

# 5. Conclusion

The aim of the thesis work was to propose new CHON ligands for the separation of americium. In particular, the work focused on the search for the best molecular structure of the ligand for the americium complexation in the aqueous phase of the AmSel process.

The synthesis of the new hydrophilic ligands and the evaluation of their extractive properties provided new insights into the feasibility of AmSel process. However, the results of this work are by no means definitive as we want to make the Amsel process industrial. To achieve this goal, not only the molecular structure can be further improved, but also the chemical synthesis as well as the conditions under which the ligand is employed.

Except for propan-1,2-diol-BTzBP which presented unexpected solubility problem since the propan-1,2-diol is more hydrophilic than ethoxyethanol, both the other proposed ligands gave promising results.

Due to the lack of time, the solubility problem of the propan-1,2-diol-BTzBP was not investigated and few tests were carried out on the other ligands. With the few data collected, ethoxyethanol-BTzBP and ethoxyethanol-BTzPhen allow to reach a SFCm/Am equal to 1.63 and 2.55, values which are comparable with the SFCm/Am equal to 2.5 of the SO3-Ph-BTBP. The most promising ligand seems to be ethoxyethanol-BTzPhen; further investigations on its behavior will be done.

The ligands under study in this work gave very positive and promising results. This does not mean that these are the definitive ligands for the AmSel process. Further research are needed to further improve the AmSel performance, making the nuclear power production more efficient and sustainable.

# References

| [1] | J. C. Slater, Atomic Radii in Crystals, The Journal of Chemical Physics, Vol.41, no. 10, 1964 |
| --- | --- |
| [2] | J. Narbutt, New trends in the reprocessing of spent nuclear fuel. Separation of minor actinides by solvent extraction, Annales Universitatis Mariae Curie-Sklodowska Lublin-Polonia, Vol. LXXI, 1, 2016 |
| [3] | M. P. Jensen, A. H. Bond, Comparison of Covalency in the Complexes of Trivalent Actinide and Lanthanide Cations, Journal American Chemical Society, 2002, Vol. 124, 33, p. 9870–9877 |
| [4] | C. Wagner, U. Müllich, A. Geist & P. J. Panak, Selective Extraction of Am(III) from PUREX Raffinate: The AmSel System, Solvent Extraction and Ion Exchange, Vol. 34, no. 2, 2016 |